## Slide 1: Study Energy Spread Cut (1) LYSO + APD
~50%
~25%
~60%
~10%
~10%
~10%
~10%
~10%
~10%
~10%
~5%
Emax
E5x5
No obvious improvement after energy spread study.

## Slide 2: Study Energy Spread Cut (2) LYSO +APD
E1x1/E3x3 < [0.25, 0.35, 0.50, 1.00]
Nor. version

## Slide 3: Study Energy Spread Cut (2) PbWO4 +SiPM
E1x1/E3x3 < [0.55, 0.70, 0.85, 1.00]

## Slide 4: Threshold Study Find DAC to Energy Mapping of CITIROC
How to find the DAC to energy mapping of CITIROC?
Set different threshold on CTIROC 220 ~ 620 (digit)
  During test beam :
  LYSO threshold = 268 ~ 300 (digit)
  PbWO4 threshold = 400 ~ 650 (digit)
Get energy spectrum with different threshold setting
Fit energy spectrum to the find the corresponding threshold in DAC(digit) to Energy(MeV) mapping
202keV
307keV
pedestal
LYSO crystal
GAGG
SiPM
CITI ROC
Set threshold
Radiation source
Get energy spectrum of LYSO
Calorimeter
DAQ

## Slide 5: PWO THR on Ch40
THR 計算過程
The function of fitting on average THR:
  Average -3375.4+15.25*x+0.017 x2+ 2500
    PS: Because in beam test data, we’ve added 2500 for prevent “-ADC”.
In PWO: Average Cal.ADC = (ADC-4572.9)/1.04
Using single channel gain: E = (Cal.ADCmax+4770)/323.47
Thus, the THR set as 400~650 is:
  DAC 400 = 7944 ADC = 24.8MeV
  DAC 600 = 14394ADC = 43.9MeV
  DAC 650 = 16219 ADC = 49.4MeV
double DAC = 400; double ADC=(-3375.4+15.25* DAC +0.017*pow(DAC,2)+2500 ); double CalADC = (ADC-4572.9)/1.04; double Ecut=(CalADC +4770)/323.47; cout<< DAC <<" "<< ADC <<" "<< CalADC <<" "<< Ecut <<endl;
DACTHR | μADCTHR | Cal.ADCTHR | ETHR(MeV)
400 | 7945 | 3242 | 24.77
600 | 14395 | 9444 | 43.94
650 | 16220 | 11199 | 49.37

## Slide 6: Threshold Study Fitting of Energy Spectrum
Total fitting function * Gaussian CDF on left hand side
  Gaussian: Pedestal, 202keV, 307keV, escape peak(OK).
  Exponential: background
DAC = 220 (digit)
DAC = 300 (digit)
DAC = 580 (digit)
圖要改, 畫mean(back), sigma(blue), fitting (red)

## Slide 7: Gaussian CDF

## Slide 8: MC Setting
Objective: Energy deposition in the crystal array
Particle: Positron (PDG ID = −21)
Beam energy: W-200 μm–30
Beam position: spread beam
Beam direction: perpendicular to ZDC surface
Experimental Setup : same as test beam
With optical photon turned on
No APD/SiPM simulation

## Slide 9: LYSO/PbWO4
ADC <=> Energy mapping, Fitting method (1)
NO threshold cut, Data/MC : Emax, E3x3, E5x5 (3)
With threshold cut (exp), Data/MC : Emax, E3x3, E5x5 (3)
With threshold cut (match), Data/MC : Emax, E3x3, E5x5 (3)
Threshold VS Resolution : Data, MC (1)

## Slide 10: PWO E-ADC mapping
1
Data/MC
Data / Scaled-MC

## Slide 11: PbWO4: 1x1 Data/MC in different energy
(Data-771)/(MCx281.72)
Data-771
MCx281.72
Data FIT
MC FIT

## Slide 12: PbWO4: 3x3 Data/MC in different energy
(Data-771)/(MCx281.72)
Data-771
MCx281.72
Data FIT
MC FIT

## Slide 13: PbWO4: 5x5 Data/MC in different energy
(Data-771)/(MCx281.72)
Data-771
MCx281.72
Data FIT
MC FIT

## Slide 14: PbWO4: 1x1 Data/MC with THR
(Data-771)/(MCx281.72)
Data-771
MCx281.72
Data FIT
MC FIT

## Slide 15: PbWO4: 3x3 Data/MC with THR
(Data-771)/(MCx281.72)
Data-771
MCx281.72
Data FIT
MC FIT

## Slide 16: PbWO4: 5x5 Data/MC with THR
(Data-771)/(MCx281.72)
Data-771
MCx281.72
Data FIT
MC FIT

## Slide 17: Threshold VS Resolution : Data, MC
1
Same graph in different art.
PbWO part was trying to apply the cut by the all setting which are used in Feb. 2025 beam test.
The magenta circle is the threshold for the analysis data, the magenta point is the “DATA”.
Do the comparison with data, the data is better then MC in THR = 30.0MeV case.

## Slide 18: Plan for the Test Beam next March
Original plan :
  PbWO4 + newSiPM + H2GCROC
New plan :
  PbWO4 + oldSiPM + CITIROC (full readout)
  PbWO4 + oldSiPM + H2GCROC
  LYSO + APD + CITIROC (full readout)
To do
Known problem for PbWO4 : threshold too high in last test beam (noisy)
CR test in Taiwan is undergoing to reduce noise
If we can fix the problem, we would like to test it again. PbWO4 + SiPM +CITIROC
Also to test w/ another DAQ, H2GCROC
Know problem for LYSO : Wrongly operation of APD

## Slide 19: CR Test

## Slide 20: Backup

## Slide 21: Threshold Study Fitting of Energy Spectrum
Fitting function:
Gaussian: Pedestal, 202keV, 307keV
Exponential: background
Gaussian CDF :
From the fitting, we can define threshold position
DAC = 220 (digit)
DAC = 300 (digit)
DAC = 380 (digit)
DAC = 460 (digit)
DAC = 540 (digit)
DAC = 580 (digit)