## Slide 1: Our Support to TiDC
ASGC (Academia Sinica Grid Computing)
Mechanical Parts Production in the workshop of IoP, Academia Sinica:
  In 2025, ~ 40 fabrication requests mainly from NTU, NCU and AS.
  1,300+ parts produced.
  Total cost: ~ NTD 2M
    50% covered by IoP, AS and 50% covered by TiDC
Radiation Tests:
  Maintain strong collaboration and good relationships with radiation test facilities in Taiwan.
  Provide hands-on support and training for research institutes and private companies on planning and conducting radiation tests for electronic components and materials.
  Explore and evaluate heavy-ion irradiation test opportunities outside Taiwan to expand testing capabilities.
    Completed one heavy-ion radiation test campaign at Texas A&M University in 2025.

## Slide 2: TASA’s SERMI Project Radiation Monitoring in Space
Chih-hsun Lin
Institute of Physics, Academia Sinica
Taiwan

## Slide 3: Goal of SERMI
Space Mission trends:
  Build smaller satellites with less resources but maintain high performance
  The use of commercial parts (COTS) in current space missions has become unavoidable.
Radiation testing is essential to ensure mission success and reliability.
How to use (limited) radiation test data to
predict in-orbit performance (failure rate)
Notes: Not a particle detector.

## Slide 4: Goal of SERMI
Link the in-orbit observation with ground test data.
Space Radiation measurement with reasonable precision.
  Particle fluence above large LET value [ ~ few MeV*cm2/mg]
  Total dosage measurement up to at least 5-10 krad (> 3 years)
A small space radiation monitoring instrument/design suitable for all kinds of missions.
  Individual payloads
  Part of satellite electronics
Minimum resource requirements.
Establish and Verify correlations between
Ground radiation test results and SEE measurements of
modern ICs in space.

## Slide 5: Design Solution
Particle fluence detector  Random-access memory (RAM)
TID detector  Devices (MOSFET) built by the CMOS process.
Many radiation tests are required.
*“The LHC accelerator radiation monitoring system,” J. Proc. Sci. [Online]
*”A New RadMon Version for the LHC and its Injection Lines”, IEEE TRANSACTIONS ON NUCLEAR SCIENCE, VOL. 61, NO. 6, DECEMBER 2014

## Slide 6: SRAM Selection and Qualification
The parallel bus Static RAM was selected:
  Straightforward upset identification and recovery.
  Simplest address decoding and R/W logics. Upsets in the address decoder could be ignored.
  Wide availability of commercial devices.
Three 1Mbit SRAMs with different part numbers were selected initially for the qualification.
Qualification criteria:
  No SEL observed in the proton beam tests.
  Low SEL cross-sections.
  Sufficient SEU cross-sections but low enough to avoid double bit flips.
200 MeV
Proton beam tests
Heavy Ion
Beam Test
15 MeV - 150 MeV
Proton Beam Test

## Slide 7: 200 MeV Proton Beam Test
Kaohsiung Chang Gung Memorial Hospital, Taiwan
200 MeV Scanning Proton Beam (10 cm x 10 cm)
Three different fluxes
  4.54x107 p/(cm2*sec)
  3.03x107 p/(cm2*sec)
  8.32x107 p/(cm2*sec)
Total Fluence=2.78x1011 p/cm2 Total Dose = 16.15 kRad

## Slide 8: SRAM SEE Detection Method
Single Event Latch up (over current):
  Current limit protect by the power supply
  Continuous current monitoring for SEL detection.
  Manual power switch
Single Event Upsets:
  Test pattern = “11110000” for all addresses
  After the initialization, the continuous dynamitic SEU test loop is
    Read  Compare  Write

## Slide 9: SRAM Proton Test Results
Chart: Run number
| 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26 | 27 | 28 | 29 | 30 | 31 | 32 | 33 | 34 | 35 | 36 | 37 | 38 | 39 | 40 | 41 | 42 | 43 | 44 | 45 | 46 | 47 | 48 | 49 | 50 | 51 | 52 | 53 | 54 | 55 | 56 | 57 | 58 | 59
#C, 0->1 | 609 | 351 | 364 | 697 | 745 | 679 | 786 | 582 | 689 | 860 | 739 | 680 | 827 | 529 | 563 | 530 | 634 | 718 | 421 | 635 | 571 | 663 | 786 | 351 | 304 | 647 | 428 | 363 | 705 | 432 | 433 | 488 | 498 | 325 | 472 | 527 | 417 | 343 | 718 | 336 | 375 | 468 | 249 | 1298 | 1133 | 1175 | 1445 | 1426 | 1510 | 1127 | 1308 | 1565 | 1653 | 1053 | 1329 | 1165 | 1746
#C, 1->0 | 599 | 642 | 851 | 783 | 818 | 666 | 1243 | 805 | 800 | 865 | 1192 | 961 | 965 | 980 | 626 | 741 | 843 | 816 | 627 | 1127 | 477 | 1134 | 1480 | 828 | 456 | 571 | 824 | 623 | 691 | 628 | 609 | 856 | 656 | 634 | 654 | 831 | 614 | 368 | 1161 | 506 | 722 | 653 | 831 | 1849 | 1898 | 1896 | 2207 | 1676 | 2227 | 1893 | 1794 | 2202 | 1875 | 1491 | 1904 | 1745 | 2242
Chart: Proton Flux
| 45392124.530612215 | 30261416.353741478 | 83218894.972789064
#C, 0->1 | 598.25 | 452.4 | 1352.3571
#C, 1->0 | 833.6786 | 694.2667 | 1921.3571
Only one type [SRAM#C] met requirements, No SEL observed.
Average SEU Cross-sections at 200 MeV: (01)=3.190.31 x 10-7cm2/chip, (10)=4.630.37 x 10-7cm2/chip
4.54x107
3.03x107
8.32x107

## Slide 10: Heavy Ion Beam Test
Radiation Effects Facility in TAMU Cyclotron Institute, USA
Beam Energy = 24.8 MeV/u
5 test boards (10 SRAMs in total) were tested.
  Four to Six SRAMs were verified at each LET value.
Ion Selections
  40Ar, 63Cu, 84Kr, 129Xe
  LETs values (MeV*cm2/mg) = 5.59, 9.5, 13.3, 16, 19.9, 26, 32, 41.8, 40, 60
SEUs were observed across all tested LET values.
SELs were first observed at LET = 16 MeV*cm2/mg.

## Slide 11: SRAM Soft and Hard SELs
Chart: SRAM#1, LET=16, R92
Alaways 6.2% of memory bits being stuck at either “0” or “1”
Chart: SRAM#2, LET=41.8, R175
82 mA -> 102 mA for a SEL of one SRAM
No permanent damage was observed.

## Slide 12: SRAM Soft+Hard SELs – Weibull Fit and Estimated LEO Rate
(x)=A(1-exp{-[(x-x0)/W]S})
Chart: LET (MeV*cm2/mg)
| 5.6 | 9.5 | 13.3 | 16 | 19.899999999999999 | 26 | 32 | 41.8 | 50 | 60
SEL Data | 0 | 0 | 0 | 2.4986e-07 | 5.6923e-07 | 0 | 3.2017e-07 | 2.0735e-06 | 2.1798e-06 | 1.1254e-05
Use OMERE v5.9.1
  Orbit parameters:
    Apogee = Perigee = 800 km, Inclination = 98o
  Cosmic ray model: GCR ISO 15390, Solar minimum
  2 mm Al shield
Estimated SEL orbital rate:
  Weibull Fit = 0.44x10-6/day per chip
  Worse Case = 6.30x10-6/day per chip

## Slide 13: SRAM SEUs
Chart: LET (MeV*cm2/mg)
| 5.6 | 13.3 | 16
#1-2, SEU(1->0) | 0.16974 | 0.24889 | 0.25562
#1-3, SEU(1->0) | 0.27762 | 0.3663 | 0.37688
#2-2, SEU(1->0) | 0.18385 | 0.22411 | 0.2687 | 0.30117 | 0.23652 | 0.25579 | 0.24933 | 0.34649 | 0.33202
#2-3, SEU(1->0) | 0.14026 | 0.17752 | 0.20713 | 0.23046 | 0.17678 | 0.195 | 0.20191 | 0.2972 | 0.29199
#5-2, SEU(1->0) | 0.16836 | 0.19641 | 0.23442 | 0.28712
#5-3, SEU(1->0) | 0.13788 | 0.15847 | 0.20232 | 0.23933
#6-2, SEU(1->0) | 0.1793 | 0.17272 | 0.24038 | 0.25078 | 0.27811
#6-3, SEU(1->0) | 0.15085 | 0.1619 | 0.19927 | 0.21227 | 0.23772
#9-2, SEU(1->0) | 0.16362 | 0.17578 | 0.19398
#9-3, SEU(1->0) | 0.27296 | 0.26333 | 0.29837
Excluding samples #1–3, the chip-to-chip variation is about 25%.
Take: #2-2 as the worse condition. #6-3 as the best condition.

## Slide 14: SRAM SEU – Curve Fitting
(x)=A(1-exp{-[(x-x0)/W]S})
Chart: LET (MeV*cm2/mg)
| 5.6 | 9.5 | 13.3 | 16 | 19.899999999999999 | 26 | 32 | 41.8 | 50
#2-2 | 0.18385 | 0.22411 | 0.2687 | 0.30117 | 0.23652 | 0.25579 | 0.24933 | 0.34649 | 0.33202
#6-3 | 0.15085 | 0.1619 | 0.19927 | 0.21227 | 0.23772
Worse
Mean
Best
Chart: Proton Energy
 | 4.625e-07
A = 15 MeV (assumption)
B = 39.0 calculated from measurement.
Proton beam tests at low energies are planned.

## Slide 15: SRAM SEUs – estimated LEO Rate
Use OMERE v5.9.1
  Orbit parameters:
    Apogee = Perigee = 800 km, Inclination = 98o
  Models:
    Trapped Proton : AP8
    Solar Proton : ECSS 10-04
    Cosmic Ray : GCR ISO 15390
  2 mm Al shield
Estimated SEU orbital rate (/device/day):
  Sufficient to make the ground-space correlation.
Good for the monitoring of long-term variations and solar events. The sensitivity is improved by multi chips and missions.
 | CR-Ion | Proton Total | Trapped P | Solar P | CR-P
Solar Min |  | 2.760.69* | 2.43 | 0.26 | 0.07
Solar Max |  | 1.820.46* | 1.52 | 0.26 | 0.04
 | CR-Ion | Proton Total | Trapped P | Solar P | CR-P
Solar Min |  | 2.760.69* | 2.43 | 0.26 | 0.07
Solar Max |  | 1.820.46* | 1.52 | 0.26 | 0.04
*Assume 25% chip-to-chip variations for Proton SEU

## Slide 16: TID Sensors
VT01 from Varadis
  MOSFETs with 400 nm oxide thickness MOSFETs.
  Two MOSFETs in one package.
  TID ranges up to 100 krad, Max sensitivity = 0.55 mV/rad (TID dependent).
  Require constant 10A current source and ADC circuits.
  One time usage.
FGD-03F from sealicon
  Floating Gate (FG) capacitor.
  Two sensors in one package.
  Integrated IC with an SPI interface.
  Rechargeable, Sensitivity ~ 1.5-2.0 mRad
RadNan-XK from 27G
  Two sensors in one package.
  Integrated IC with an UART interface.
  TID ranges up to 10 krad, Sensitivity = 0.1 mRad.
  One time usage.

## Slide 17: 200 MeV Proton Radiation Test
Kaohsiung Chang Gung Memorial Hospital, Taiwan on 2025/11/15.
200 MeV Scanning Proton Beam (15 cm x 15 cm)
53 (49) runs in total Flux = 1.116x107 p/(cm2 *sec) Fluence = 5.694x1010 p/cm2
Total Dose = 3.305 kRad (at least 3-5 years in LEO)
Dose per run = 64.612% Rad

## Slide 18: RadNano-XK TID Measurement
30 seconds per measurement
Dose = 64.612% Rad per run

## Slide 19: RadNano-XK TID Measurement
RadNano#1 : 59.141.91 Rad (92%)
RadNano#2 : 62.321.30 Rad (96%)
LSB = 0.1 mRad

## Slide 20: FGD-03F TID Measurement
Target = 90 kHz, Threshold = 50 kHz
Charging time ~ 3 seconds

## Slide 21: FGD-03F TID Measurement
FGD#1: 2.430.06 mRad/Hz, FGD#2: 2.300.06 mRad/Hz
Additional tests are required to confirm the accumulated dose/dose rate dependence effect
Dose = 64.612% Rad per run

## Slide 22: VT01 TID Measurement
Noticeable discharging effects were clearly observed during the measurements.

## Slide 23: VT01 TID Measurement
Good agreement with the calibration curve was observed with the non-linear response:
  LSB ~ 49.3 mRad at the beginning.
  LSB ~ 105.2 mRad after 3.3 kRad irradiation.
Only sensitive to solar events.
Sum of V between irradiation
Dose = 64.612% Rad per run

## Slide 24: SERMI for CubeSat Missions
SRAM
SRAM
FPGA
RADNano
FGD
VT01
Power
TMTC
PPS
10 cm
Input power = 15-5V, Average Power = 0.37W
UART with RS422 for TM/TC.
PPS with RS422 for the measurement time.
JTAG
P & T
Monitor
ADC for VT01

## Slide 25: Summary
The SERMI payload for the CubeSat mission has been completed.
Launch is planned on two CubeSats later this year.