## Slide 1: ZDC Crystal ECAL Development 20260501 @ ePIC General Meeting
Chia-Yu Hsieh
Institute of Physics, Academia Sinica, Taiwan
on behalf of the ZDC Crystal ECAL Group

## Slide 2: ZDC Design
ECAL
LYSO Crystal
20*20 cells
3cm*3cm*7cm / cell
60cm*60cm
7cm ~ 6.5X0 in Z
HCAL : sampling calorimeter
1 layer = steel + scintillator tile + SiPM
64 layers, 8 slice/layer
65cm in X, 60cm in Y, 163cm in Z
Beam line
ZDC = ECAL + HCAL
ECAL
crystal calorimeter
provide good energy resolution
HCAL
Sampling calorimeter
provide good position resolution
Requirements of energy resolution are for hadrons and photons are 50%/sqrt(E) + 5% and 20%/sqrt(E) + 5%, respectively. Furthermore, ECAL has sensitivity to photon down to 100 MeV.

## Slide 3: 1st Prototype of ZDC ECAL
Onsemi SiPM
LYSO crystal
(8x8 , 8X0, ESR)
CITIROC (160-400pC)
 | Detector | Crystal |  |  |  | Sensor |  | DAQ
 |  | name | Size of one cell | Length | Array | Type | Sensor /crystal | 
1st prototype 2023-2024 | LYSO + SiPM | LYSO | 0.7cm*0.7cm | 8cm (8X0) | 8x8 | SiPM Onsemi MICROFC-60035 | 1 | CITIROC

## Slide 4: CITIROC DAQ
LYSO +SiPM (64ch)
CITIROC_A (32ch) CITIROC_B (32ch)
Low voltage (12V)
SpaceWire Mk4
UART
Laptop
Data taking
Control
Monitor
Data
Control
Temperature
CITIROC is a 32-channel front-end ASIC designed to readout silicon photo-multipliers.
Dynamic range up to 400pC
Shaper
Peak Sensenig ADC
Data, slow control (threshold, gain, etc setup), online monitoring (DAQ deadtime, temperature) are all through laptop interface.
CITIROC spec.

## Slide 5: 1st Prototype : SiPM Saturation
Test beam at RARiS on 2024 Feb, using 50MeV - 800MeV positron beam.
Most of data points lying in the non-linear region
only the 47 MeV data set retaining about 60% of events within the linear range.
50-800 MeV
positron beam
Non-linearity

## Slide 6: 1st Prototype : Selection Criteria
Cut Criteria
2.5 MeV < Eₘₐₓ < 20 MeV
  Selects data within the linear response range.
  Removes low-momentum photons originating from the beam.
Both Left and Right Crystals Fired
  Requires hits in both FEE-left and FEE-right channels.
  Eliminates events containing only noise.
Beam profile @ 47MeV
FEE left
FEE right
clustering

## Slide 7: 1st Prototype : Data and MC Comparison
The comparison between data and MC for the 47 MeV positron beam shows good overall consistency.
clustering

## Slide 8: 1st Prototype : Energy Resolution w/o Energy Regression
Energy resolution without energy regression is 14% for the 47 MeV beam. After accounting for the beam momentum resolution provided, the energy resolution improves to approximately 11%.
47MeV positron
E5x5
Data
Fettig
Energy resolution of 47MeV momentum resolution = 11.6%

## Slide 9: Design of 2nd Prototype
Material | Light yield (photons/MeV) | Relative to LYSO
LYSO | ~32,000 – 38,000 | 1.0
PbWO₄ | ~200 – 400 | ≈ 1/100 of LYSO
Sensor | Typical Gain | Relative
SiPM | ~10⁵ – 10⁶ | 1.0
APD | ~10² – 10³ | ≈ 1/1000 – 1/10,000 of SiPM
Choice of crystal
Choice of sensor
1st prototype @ 2023-2024 : LYSO + SIPM, saturation
2nd prototype @ 2024-2025 : reduce the gain.
LYSO + APD
The gain of an APD is about 1000 times lower than that of a SiPM.
PbWO₄ + SiPM
The light yield of PbWO₄ is about 100 times lower than that of LYSO.
We continue using CITIROC as DAQ system.

## Slide 10: 2nd ZDC ECAL Prototype
 | Detector | Crystal |  |  |  | Sensor |  | DAQ
 |  | name | Size of one cell | Length | Array | Type | sensor/crystal | 
2nd prototype 2024-2025 | LYSO + APD | LYSO | 1cm*1cm | 6.6cm (6X0) | 8x8 8cm*8cm | APD C30739ECERH | 1 | CITIROC
 | PbWO4 + SiPM | PbWO4 | 2cm*2cm | 5.3cm (6X0) | 6x6 12cm*12cm | SiPM Onsemi MICROFC-60035 | 2 | CITIROC
LYSO + APD
PbWO4 + SiPM
Beam Monitor

## Slide 11: 2nd Prototype : Test Beam
50-800 MeV
positron beam
Beam monitor
LYSO + APD
PbWO4+SiPM
50-800MeV positron beam
We add beam monitor system in order to evaluate position resolution.

## Slide 12: 2nd Prototype : Linearity
APD HV
405 V
395 V
385 V
LYSO + APD
Linearity: The detectors showed good linearity when tested with an electron beam from 50 MeV to 800 MeV.
SiPM HV
32.6V
PbWO4 + SiPM

## Slide 13: 2nd Prototype : Energy Resolution (w/o Energy Regression)
LYSO + APD (APD=405V)
LYSO + APD : Poor performance ~ 35% energy resolution with 700MeV positron beam.
PbWO4 + SiPM : Reasonable performance ~ 15% energy resolution with 700MeV positron beam.
The energy regression is not performed.
PbWO4 + SiPM (SiPM=32.6V)

## Slide 14: Residual of “PbWO4 + SiPM”
Position resolution
Since the resolution of BMs (2mm pitch) are very small compared PbWO4 crystal (2cm pitch). The position resolution ~6.5mm is mostly from PbWO4 crystal itself.
PbWO4 system @ 739 MeV
Residual
Residual in X
Residual in Y

## Slide 15: Performance of “PbWO4 + SiPM”
Energy resolution
Position resolution
For 2nd prototype, only PbWO4 + SiPM system gives reasonable performance.
  Energy resolution : ~15% @ 800MeV positron beam
  Position resolution : ~ 6.5mm @ 800MeV positron beam
Satisfy the requirement, but we need to measure with higher energy beam to have full picture.
(Chi2/NDF = 13.56/6)

## Slide 16: MC Simulation Condition
BM2
BM1
PbWO4
50MeV ~ 796 MeV positron beam
Beam spread
perpendicular beam
gaussian random
Center (x, y) = (11.4, -4.98) mm
Sigma (x, y) = (-4.98, 8.62) mm
PbWO4 crystal array is shifted
(x, y) = (10, -1) mm, compare to alignment

## Slide 17: Beam Profile
BM1
Profile in X
Profile in Y
BM2
Nice consistency

## Slide 18: ADC to MeV Conversion
  Data (ADC) = MC (MeV) * 370.73 + 8417

## Slide 19: Data and MC Comparison : Emax
Nice consistency except for 98MeV because of 50MeV threshold cut

## Slide 20: Data and MC Comparison : E5x5 w/o threshold cut

## Slide 21: Data and MC Comparison : E5x5 w/ threshold cut

## Slide 22: Data and MC Comparison : Energy Resolution (sigma)
Notice that MC and Data are w/o energy regression.
But they both satisfied the requirement.
Performance of MC is around 2% better than Data.
We might need to push to higher beam energy to see >1GeV performance.

## Slide 23: Data and MC Comparison : Position Resolution (sigma) and Bias (mean)

## Slide 24: Photon Sensors
Onsemi SiPM (MICROFC-60035) : https://www.onsemi.com/pdf/datasheet/microc-series-d.pdf
Hamamatsu SiPM (S14160-3015PS) : https://www.hamamatsu.com/us/en/product/optical-sensors/mppc/mppc_mppc-array/S14160-3015PS.html
Feature | onsemi SiPM (MICROFC-60035) | Hamamatsu SiPM (S14160-3015PS)
Active area | 6 × 6 mm² | 3 × 3 mm²
Gain | ~10⁶ | ~10⁶
Bias voltage | ~24–30 V | ~38–55 V
PDE (peak) | ~40–50% | ~45–55%
Dynamic range (p.e.) | 1 – ~1.5×10⁴ p.e./cell 527 cells/mm² | 1 – ~3×10⁴ p.e./cell 4,443 cells/mm²
Limiting factor | Microcell saturation | Microcell saturation
Next prototype, we will move to Hamamatsu SiPM.
Smaller area (more microcells per unit area) and larger dynamic range gives the Hamamatsu SiPM better linearity than the onsemi device. We expect to keep the linearity up to 29 GeV.

## Slide 25: CITIROC VS H2GCROC
CITIROC
Dynamic Range: 160 fC – 400 pC
Per-Channel Bias Control: 0–4 V, 8-bit DAC for SiPM gain equalization
Dual-Gain Preamplifier:
  Low Gain: ×1–×60
  High Gain: ×10–×600
  (higher resolution, smaller range)
Signal Shaping
Self trigger
Automatic Gain Selection: Auto HG/LG switching or LG-only mode
H2GCROC
Dynamic Range: 160 fC – 320 pC
Digitization:
  10-bit ADC @ 40 MHz (integrated charge)
  12-bit TOA (TDC 24 ps)
  12-bit TOT (TDC 50 ps)
  If ADC is saturated, then automatically switch to TOA and TOT mode.
Trigger & Data Flow:
  FPGA supports self-trigger or external-trigger mode
H2GCROC

## Slide 26: 3rd Prototype : Mechanical Support
Add H2GCROC
Potentially adding one more BM.
Add shielding boxes for all electronics.
CITIROC
H2GCROC

## Slide 27: 3rd Prototype : new SiPM Board
Location of laser and receiver?

## Slide 28: Planning for 3rd Prototype
 | Detector | Crystal |  |  |  | Sensor |  | DAQ
 |  | name | Size of one cell | Length | Array | Type | sensor/crystal | 
1st prototype 2023-2024 | LYSO + SiPM | LYSO | 0.7cm*0.7cm | 8.8cm (8X0) | 8x8 | SiPM Onsemi MICROFC-60035 | 1/crystal | CITIROC
2nd prototype 2024-2025 | LYSO + APD | LYSO | 1cm*1cm | 6.6cm (6X0) | 8x8 | APD C30739ECERH | 1/crystal | CITIROC
 | PbWO4 + SiPM | PbWO4 | 2cm*2cm | 5.3cm (6X0) | 6x6 | SiPM Onsemi MICROFC-60035 | 2/crystal | CITIROC
3rd prototype 2025-2026 (developing) | PbWO4 + SiPM | PbWO4 | 2cm*2cm | 5.3cm (6X0) | 6x6 | SiPM Hamamatsu S14160-3015PS | 16/crystal | CITIROC HGCROC
The 3rd prototype will use the same crystals
  SiPM will be changed from Onsemi → Hamamatsu
  DAQ will be upgraded from CITIROC → H2GCROC
Possible test beam opportunities:
  DESY in Germany @ June : 1GeV - 6GeV electron/positron beam
  RARiS in Japan @ July : 50MeV - 1 GeV electron/positron beam
System to be tested in the coming test beam
  PbWO4 + Onsemi SiPM board + CITIROC : reduce noise and test again
  PbWO4 + Onsemi SiPM board + H2GCROC : 1st try to use H2GCROC
  PbWO4 + Hamamatsu SiPM board + H2GCROC : test new SiPM board + new DAQ system
  LYSO + Hamamatsu SiPM board + H2GCROC : redo LYSO

## Slide 29: Lab Test of H2GCROC
Pedestal calibration (OK)
Decoding (OK)
Gain calibration with LYSO + SiPM + H3GCROC : connector issue (pending)
CR test with LYSO + SiPM + H3GCROC : connector issue (pending)

## Slide 30: Plan for Final Design
Super module
Crystal : PbWO4
SiPM : S14160-3015PS_HAMAMATSU
One crystal = 20.5 mm*20.5 mm*7.0 mm (7.87 X0)
Active area = 59cm*59cm
One Super Module (SM) = 9 x 9 crystals
Num. of crystals = 3x3 SMs = 729 crystals
16 SiPMs / crystal
Num. of SiPMs = 729 * 16 = 11, 664

## Slide 31: Plan for Final Design : Frame
Cooling & support
Crystal modules
PCB support
SiPM PCB + ROC PCB

## Slide 32: Plan for Final Design : PCB

## Slide 33: Plan for Final Design : Cooling
Copper plate
T=3 mm
Heat flow simulation is undergoing.

## Slide 34: Backup

## Slide 35: To Do List for Coming Test Beam
PbWO4 + Onsemi SiPM board + CITIROC : reduce noise and test again
  Data analysis (online plot) : Done
  Data and MC comparison : Done
  New mechanical support : Done
  Noise test : Done
  BM calibration : Done
  CR test : Analysis undergoing
PbWO4 + Onsemi SiPM board + H2GCROC : 1st try to use H2GCROC
  Data analysis (online plot) : Undergoing
  Mechanical support : Undergoing
  LED test (SiPM gain calibration) : Undergoing
  External trigger from two BM systems : Undergoing
  Radiation source test (ADC to Energy conversion) : To do
  CR test : To do
PbWO4 + Hamamatsu SiPM board + H2GCROC : test new SiPM board + new DAQ system
  SiPM board layout and production : Undergoing
  Data analysis (online plot) : Undergoing
  Mechanical support : Undergoing
  LED test (SiPM gain calibration) : To do
  Radiation source test (ADC to Energy conversion) : To do
  CR test : To do

## Slide 36: Noise Test and Cosmic Ray Test
BM1
CR test setup @ NCU
BM2
LYSO
PbWO4
BM1/BM2/LYSO/PbWO4 all have several components need to be grounded.
Box for crystal/scintillators
Ground of SiPM board
Ground of GTM board (CITIROC)
Box of MK4 module (data stream)
Box of UART module (slow control)
Support frame
BM1/BM2
LYSO/PbWO4
GTM (2*CITIROCs)
Power supply(12V)
Mk4
UART
Laptop
Data
Control
Grounding choices
Negative bias of power supply
Ground of power supply
Ground from the wall
Noise level is currently at 12 MeV ~ 18MeV. During 2025 test beam, it was 50 MeV.

## Slide 37: Beam Monitor Calibration
Before
After
Position 1
Y-axis
X-axis
Flux
Flux
Position 2
Position 3
Using flux of 22Na source to do the beam monitor calibration.
Flux distribution results with source placed at different positions after calibration
d
r

## Slide 38: CR Analysis?