## Slide 1
Ring Contact Technology and Sputtering Technology
Kunming Dong
PIRE GEMADARC Collaboration Meeting 2023
June 2nd, 2023

## Slide 2
Sputtering Technology with Thin contacts
Background and Motivation
Current Experimental Progress
Future Plan
Summary
Outline
Ring Contact Technology
Background and Motivation
Current Experimental Progress
Future Plan

## Slide 3: Objective
n+ contact
P+ contact
Project Goal: To advance novel GeRC detector technology to study the feasibility of using large-size Ge detectors for LEGEND-1000. To achieve this goal, the following three objectives are determined:
  Fabricate the first GeRC detector with a mass of ~2 kg from an existing USD-grown crystal. The fabrication will be conducted at TAMU in collaboration with Prof. Rusty Harris and William Baker.
  If the detector is successful, we will investigate the energy resolution and pulse shape properties of this detector. The characterization will be conducted at UNC in collaboration with Prof. John Wilkerson.
  Grow a new crystal with a mass of >3 kg at USD for fabrication and characterization of the second GeRC detector.
Cross section of GeRC Detector as proposed by David Radford, ORNL

## Slide 4: Design based on Simulation
Detector Capacitance Prediction
Ring Contact Length (mm) | Predicted Capacitance by Siggen (pF) | Depletion Voltage (V)
4 | 25.0 | 1347
3 | 22.7 | 1370
2 | 20.2 | 1381
1 | 16.9 | 1374
0.5 | 14.5 | 1352
Cross-section view of the detector.
Predicted detector capacitance with different ring sizes by Siggen.
Ring Contact Width: 1 mm
Depletion Voltage: 1374 V
Applied Voltage: 2500 V

## Slide 5: Mechanical Processing
Grinding
Thickness: 28.1mm
Δ thickness: <0.3mm
Core Drilling (Cylinder)
Radius: 25.3 mm
Cutting Groove
Groove:
Bottom Depth: 8.4 mm
Bottom Radius: 16.9 mm
Bottom Length: 4.1 mm
Gap at Outer Radius: 10 mm
Core Drilling (Hole)
Radius: 9.8 mm

## Slide 6: Surface Treatment
Sanding
With graduated fineness of grinding media (sandpaper)
Lapping
17.5 um powder for coarse lapping
9.5 um powder for fine lapping
Polishing
1 um and 0.3 um polishing powder

## Slide 7: Cleaning and Etching
Acetone- 2 mins
Isopropyl Alcohol- 2 mins
Methanol- 2 mins
4. Trichloroethylene- 2mins
5. Acetone- 2 mins
6. DI water- 2 mins
RCA Cleaning
5% HF and 95% HNO3
30 seconds
Heavy Etching

## Slide 8: Contacts Fabrication
Lithium Diffusion
Deposition
Al Deposition

## Slide 9: Future Plan
Output from Julia:
Calculated capacitance at 5000 V: 23.3 pF
Depletion voltage: ~4400 V
Input:
Impurity concentration: (2.06 ~2.94) 1010/cm3
Applied bias voltage: 4000 V on the n+ contact.
The same height and radius as the real crystal.
Hole diameter: 20 mm
  Refabricate GeRC detector #0.
  Fabricate the GeRC detector with a mass of ~2 kg from an existing USD-grown crystal. The fabrication will be conducted at TAMU in collaboration with Prof. Rusty Harris and William Baker.
  If the detector is successful, we will investigate the energy resolution and pulse shape properties of this detector. The characterization will be conducted at UNC in collaboration with Prof. John Wilkerson.
  Grow a new crystal with a mass of >3 kg at USD for fabrication and characterization of the second GeRC detector.

## Slide 10: Project Goal
Project Goal: To advance contact technology for studying the feasibility of using large-size Ge detectors for rare-event physics searches. To achieve this goal, the following four objectives are determined:
Purchase a larger and more advanced automated sputtering system
Find out the impact of different parameters on contact through many tests. Then find recipes for different types of detectors
Fabricate small detectors to characterize the contact performance produced by the new sputtering system
Design and fabricate large-size detectors

## Slide 11: HPGe Detector Fabrication Introduction
Desired electrical contact characteristics:
A n+ contact blocks hole injection
A p+ contact blocks electron injection
Withstand high fields ~ few kV/cm
Mechanically robust
Thin dead layer
Stable characteristics with time, T cycling, and environmental exposure
Desired surface passivation characteristics:
Low surface leakage
Charge neutral
Withstand high fields ~ few kV/cm
Mechanically robust
Thin dead layer
Stable characteristics with time, T cycling, and environmental exposure

## Slide 12: Sputter Deposition Technology
What is sputtering?
  Sputter deposition is a physical vapour deposition (PVD) method of depositing thin films by sputtering material from a ‘target’, then depositing it onto a ‘substrate’.
Process of sputtering
  The principle of sputtering is to use the energy of a plasma (partially ionized gas) on the surface of a target (cathode), to pull the atoms of the material one by one and deposit them on the substrate.

## Slide 13: Temperature variation during sputtering
Temp Measurements
Power | Time (min) | Temp(℃)
RF-150W | 30 | Less than 38
DC-400W | 7 | Less than 38
RF-480W | 5 | <38
RF-480W | 10 | 52-65.5
RF-480W | 15 | 65.5-79
RF-480W | 30 | 65.5-79

## Slide 14: Sputtering Rate
Alpha-Step Profiler
Power | Thickness(nm)
75 | <50
100 | <50
125 | <50
150 | 41
200 | 55
250 | 111
350 | 125
500 | 301
RF power, 15 mins, 30mTorr(7% H_2)
DC power, 5 mins, 3mTorr(Ar)
Power | Thickness(nm)
100 | <50
150 | <50
200 | <50
250 | 66
300 | 81
400 | 86

## Slide 15: Thickness Map
200W RF power, 30 mins
Target material: Ge
Pressure: 3mTorr(7% H_2)
Tilt angle: 10 mm
Substrate height: 2.7 inch
z=[ 473 485 473 453 461
476 475 469 473 471
467 469 470 466 455]; #nm
Film Uniformity: 3%

## Slide 16: Amorphous-Ge Film Resistivity
+V
A
Al
a-Ge
Temp (K) | Resistivity (Ωcm)
300 | 16000
30 mTorr (7% H_2)
3 mTorr (7% H_2)
Chart: Resistivity (Ωcm) vs Temp (K)
| 300 | 177 | 179 | 160 | 150 | 136 | 126 | 118.3 | 109.5 | 98 | 90 | 85 | 83 | 82 | 81.2 | 80.5
Resistivity (Ωcm) | 16 | 304054.0541 | 318181.8182 | 333333.3333 | 337837.8378 | 340599.455 | 341530.0546 | 343406.5934 | 348189.415 | 366568.915 | 425170.068 | 586854.4601 | 791139.2405 | 984251.9685 | 1344086.0215 | 1923076.9231
K
Ωcm

## Slide 17: High Purity Ge-68 Planar Detector
The HP-Ge68 detector made by Sanjay Bhattarai
The HP-Ge68 detector made by Mathbar Singh Raut
Chart: Leakage Current (pA) vs Bias Voltage (V)
| 50 | 100 | 200 | 300 | 400 | 500 | 600 | 650 | 700 | 800 | 900 | 1000
Leakage Current (pA) | 30 | 28 | 28 | 37 | 52.5 | 79.5 | 95 | 140 | 162 | 224 | 325 | 416
While the a-Ge film has low resistivity at low chamber pressure, it does not perform well in blocking holes.
Mark's experiment shows that increasing chamber pressure can improve the hole barrier height.
V
pA
Amman, Mark. (2018). Optimization of Amorphous Germanium Electrical Contacts and Surface Coatings on High Purity Germanium Radiation Detectors. 10.13140/RG.2.2.34748.08327/1.

## Slide 18: Research Plan
Use Mark Amman’s experimental data as a reference. By controlling variables, try to find parameters suitable for new sputtering systems:
Power
Coating time
Pressure
Target’s angle
Distance between target and substrate
To complete this task:
Measure resistivity under different conditions
Fabricate point contact detector and measure the charge carrier injection
Amman, Mark. (2018). Optimization of Amorphous Germanium Electrical Contacts and Surface Coatings on High Purity Germanium Radiation Detectors. 10.13140/RG.2.2.34748.08327/1.

## Slide 19: Summary
Project Goal: To advance contact technology to study the feasibility of using large-size Ge detectors for neutrinoless double-beta decay and dark matter experiments.
Done:
  The AJA sputtering system was assembled and operated successfully
  On-site training
  Temperature measurement
  Sputtering rate measurement
  Partially resistivity measurement
Chamber pressure has a great effect on the resistivity of a-Ge film
It takes a lot of experimentation to find the right recipe

## Slide 20: End
Thank you!