## Slide 1: Implementing JPA in the TASEH Axion Detection Chain
洪偉晟 (Wei-Cheng Hung),張景陽 (Jing-Yang Chang)
Advisor : 陳永富(Yung-Fu Chen), 張元翰(Yuan-Hann Chang)
JPAs team ,Low Temperature Physics Lab, NCU
Taiwan Axion Search Experiment with Haloscope, NCU&AS

## Slide 2: Axion Detecting Sensitivity
parameter | Remarks
 | Signal to noise ratio
 | Typical axion signal power
 | Average noise power
 | Effective system noise temperature
 | Resolution bin width
 | Amount of data
SSE | Scan
parameter | Remarks
 | Signal to noise ratio
 | Typical axion signal power
 | Average noise power
 | Effective system noise temperature
 | Resolution bin width
 | Amount of data
SSE | Scan
Cavity & Magnet
JPA & data taking strategy
The efficiency of reducing
  factor of 1
  : factor of square root
Hsin Chang et al, Phys. Rev. Lett. 129, 111802 (2022)
From TASEH CD102 result :
After integrating JPA in detection chain
(with the same data taking time)
Notes: To explore the importance of the parametric amplifier is, we start from the axion detecting sensitivity. The axion sensitivity are proportional to the SNR. To improve the SNR, we commence from two parts . The design of the cavity try to enhance the signal power received by the cavity. The denominator determine by the system noise power. The JPA is the device can significantly reduce the system noise by reasonable gain and quantum limited add noise.

## Slide 3: Noise in Amplification/Detection Chain
Noise power after sequential Amplifiers:
JPAs
HEMT
post
post
post
parameter | Remarks
 | Gain from amplifier
 | Add noise from amplifier
 | Effective noise temperature
parameter | Remarks
 | Gain from amplifier
 | Add noise from amplifier
 | Effective noise temperature
Amplification chain

## Slide 4: Potential Noise Source in Amplification Chain
JPAs
HEMT
post
post
post
Input noise
Thermal noise
  Neglected (~20mK environment)
noise
  Neglected (working frequency ~GHz)
Vacuum noise
  The dominated input noise source
JPA add noise
Electrons related noise
  Electrons are condensate to cooper pairs(superconductivity)
Vacuum noise
  The dominated add noise source
HEMT add noise
Suppressed by gain from previous stage amplifier
Post add noise
Suppressed by gain from previous stage amplifier
Maintaining the cryogenic Temperature 20mK helps suppress the noise generated by electrons.

## Slide 5: Emitted Noise From Black Body Source
: physical Temperature
(quantum fluctuation)
Remarks
half photon energy
*24mK/GHz (5GHz->120mK)

## Slide 6: Standard-Quantum-Limited System Noise
Amplifier | Gain (dB) | Add noise (K) | Remarks
JPA | 20 | ~0.3 | 
HEMT | 40 | ~2 | Commercial product
Post | 60 | ~100 | Commercial product, triple stages

## Slide 7: JPA Added Noise
SNR improvement
reduce detection time by a factor of
()
0.21K~1 photon

## Slide 8: Josephson Parametric Amplifier
Effective capacitor
Josephson Junction
Si
Al
Al
AlOx
JJ current phase relation :
JJ voltage phase relation :
Critical current : for

## Slide 9: Bridge Free Junction Fabrication Technique
Z. Ke et al., Chin. Phys. B 26, 078501 (2017)
Si
Al
Al
AlOx
Si
Al
Si
Al
AlOx
1st Al deposition
Deposited Al oxidization
2nd Al deposition

## Slide 10: All E-beam Lithography
Resist application
SC exposure
LC exposure
development
PR: AR-P 617.06
PR: AR-P 6200.13
Beam current: 1nA
Spot distance: 10nm
Beam current: 40nA
Spot distance: 230nm
TR: AR 600-546
BR: XAR 600-50/2
Elionix ELS-7000 | 
Accelerating voltage | 100 keV
Beam current | 10 pA – 70 nA
Minimum dose time | 50 ns/dot
Writing field size | 75, 150, 300, 600, 1200 µm
Field dot number | 20000, 60000, 240000
resources and support are from the Quantum Materials Shared Facilities of Institute of Physics at Academia Sinica.

## Slide 11: Deposition & Lift-off
1st Al deposition
2nd Al deposition
Lift off
Final pattern
Incident Angle: 25
Thickness : 30nm
Incident Angle : 25
Thickness : 60nm
Blue: 1st Al layer
Brown: 2nd Al layer
JJ area : ~0.5*0.5um2
target RT resistance: 300
AdNaNo JEB diamond | 
E-gun based pressure | 3e-9 torr
Accelerating voltage | 10kV
Oxidation based pressure | 3e-10torr
O2 Flow control | 4-220 sccm
O2 pressure control | 0.04 to 1 torr ( dynamics & statistics)
resources and support are from the Prof. Chii-Dong Chen’s lab, IoP, AS

## Slide 12: JPA Tune Up Process Flow
Flux dependence
Gain and Noise mapping
optimization
Saturation power
Operations
0.5 day
0.5 day
4 days
3 days
In total 8 days
Key parameters
Maximum resonance
Junction properties
Flux quantum with current
Key parameters
Signal Saturation power
Pump power limitation
Key parameters
Gain
Bandwidth
Operation range
Key parameters
System noise
On/off noise
Key parameters
Frequency matching
Best SNR
Implementation
Qubit readout chain
Axion detection chain
Noise squeeze
Remarks :
Full characterization ~8 days
Tune up JPA ~2days

## Slide 13: Operation Range for FDL4B8d2
Criteria of gain
18dB gain
2MHz BW
-> 400MHz covering range
-> optimized gain shows under the trade off btw duffing & flux nonlinearity

## Slide 14: Continuous JPA Operation Mapping
Covering Searching range for ~200MHz
With JPA gain BW~2MHz
BW: 2MHz
Span :600kHz
shift :0.5MHz
:20kHz
shift :1MHz
Sweeping f range :40MHz

## Slide 15: Static Magnetic Field Shielding
Goal: reduced by a factor of 103
JPA shielding set

## Slide 16: Shielding Sets Field Reduction Capacity
Magnetic Field(~500G)
Hall sensor
Shield
Torrance of leaked field
->2e-15/1e-10 (T)
-> 0.1G

## Slide 17: Current Status of JPA in TASEH Research
Adjusted target range
About JPA
New wider BW devices working around 2 GHz
Continue tuning procedure to cover ~100MHz span
About shielding
Stronger solder joint for compensate current survive above 4T
reduce the field strength lower than 0.1G

## Slide 18: Josephson Parametric Amplifier
parameter | description
 | Geometric capacitance
 | Josephson inductance
 | Shunt capacitance
parameter | description
 | Geometric capacitance
 | Josephson inductance
 | Shunt capacitance
Remarks
JPA is a nonlinear oscillator based on the Josephson junctions, nonlinear inductor , and a linear capacitor
Taylor expansion of , Quantum description
RWA:
JPA can be modeled as Duffing oscillator/ an oscillator with Kerr effect

## Slide 19: Retrieving Output Mode in JPA Dynamics
Internal thermal bath
On chip
External thermal bath
Quantum Langevin equation:
B.C.
The output mode are contributed by 4 modes

## Slide 20: Standard Quantum Limited Noise
+ +
Internal thermal bath
On chip
External thermal bath
0 :
0 :
0 :
0 :
Fine thermal equilibrium
superconductivity
From theoretical prediction , JPA could only add half photon noise, system noise could be 1 photon strength (half from vacuum, half from complex conjugated mode.